PRODUCT DESCRIPTION
CUSTOMER:  AGRIGEL
PART NAME:  CHECK VALVE BODY MALE
PART NUMBER:  LFC101
MATERIAL:  30% GLASS FILLED POLYPROPYLENE
SUPPLIER:  PLASTAMID/ADVANCED POLYMERS
MATERIAL CODE: PH2120  
COLOUR:  GREEN
 PIGMENT NUMBER AND SUPPLIER:  PERFORMANCE MASTERBATCH JP6089
WEIGHT:  37 G
NUMBER OF CAVITIES:  2
CYCLE TIME:  40 SEC
PACKAGING:  
MACHINE:  90 TON +

MOULD LOCATION:  
COMMENTS:  
