PRODUCT DESCRIPTION
CUSTOMER:  AGRIGEL
PART NAME:  EOL CV POPPET SEAT
PART NUMBER:  LFC104
MATERIAL:  30% GLASS FILLED POLYPROPYLENE
SUPPLIER:  PLASTAMID/AP
MATERIAL CODE:  PH2120
COLOUR:  GREEN
 PIGMENT NUMBER: JP6089 
SUPPLIER:  PERFORMANCE
WEIGHT:  1.8 G
NUMBER OF CAVITIES:  1
CYCLE TIME:  20 SEC
PACKAGING:  
MACHINE:  20 TON

MOULD LOCATION:  
COMMENTS:  
