PRODUCT DESCRIPTION
CUSTOMER:  AGRIGEL
PART NAME:  T PIECES
PART NUMBER:  LFC1059
MATERIAL:  30% GLASS FILLED POLYPROPYLENE
SUPPLIER:  PLASTAMID/AP
MATERIAL CODE: PH2120
COLOUR:  YELLOW
 PIGMENT NUMBER AND SUPPLIER:  JP3345 PM
WEIGHT:  14.5
NUMBER OF CAVITIES:  1
CYCLE TIME:  40 SEC
PACKAGING:  
MACHINE:  90 TON +

MOULD LOCATION:  
COMMENTS:  RUNS IN SAME MOULD AS ELBOW, HAS HYDRAULIC CORES
