PRODUCT DESCRIPTION
CUSTOMER:  AGRIGEL
PART NAME:  ELBOWS
PART NUMBER:  LFC1060
MATERIAL:  30% GLASS FILLED POLYPROPYLENE
SUPPLIER:  PLASTAMID/AP
MATERIAL CODE:  PH2120
COLOUR:  YELLOW
 PIGMENT NUMBER AND SUPPLIER:  JP3345 PM
WEIGHT:  11.5 G
NUMBER OF CAVITIES:  1
CYCLE TIME:  40 SEC
PACKAGING:  
MACHINE:  90 TON +

MOULD LOCATION:  
COMMENTS:  SAME MACHINE AS T-PIECES, HAS HYDRAULIC COURSE
