PRODUCT DESCRIPTION
CUSTOMER:  AGRIGEL
PART NAME:  EOL CV ADJUSTABLE BARB
PART NUMBER:  LFC108
MATERIAL:  30% GLASS FILLED POLYPROPYLENE
SUPPLIER:  PLASTAMID/ADVANCED POLYMERS
MATERIAL CODE:  PH2120
COLOUR:  GREEN
 PIGMENT NUMBER AND SUPPLIER:  JP6089 PERFORMANCE MASTERBATCH
WEIGHT:  14.0 G
NUMBER OF CAVITIES:  2
CYCLE TIME:  30 SEC
PACKAGING:  
MACHINE: 90 TON +

MOULD LOCATION:  
COMMENTS:  
