PRODUCT DESCRIPTION
CUSTOMER:  AGRIGEL
PART NAME:  EOL CV LOCK NUT
PART NUMBER:  LFC109
MATERIAL:  30% GLASS FILLED POLYPROPYLENE
SUPPLIER:  PLASTAMID/ADVANCED POLYMERS
MATERIAL CODE: PH2120
COLOUR:  GREEN
 PIGMENT NUMBER AND SUPPLIER:  JP6089 PERFORMANCE MASTERBATCH
WEIGHT:  3.0G
NUMBER OF CAVITIES:  2
CYCLE TIME:  40 SEC
PACKAGING:  
MACHINE:  90 TON +

MOULD LOCATION:  
COMMENTS:  UNSCREW BY HAND
