PRODUCT DESCRIPTION
CUSTOMER:  AGRIGEL
PART NAME:  FILTER BODY
PART NUMBER:  LFF101
MATERIAL:  POLYPROP
SUPPLIER:  SASOL
MATERIAL CODE:  2448PC
COLOUR:  NATURAL
 PIGMENT NUMBER AND SUPPLIER:  
WEIGHT:  346.8 G
NUMBER OF CAVITIES:  1  
CYCLE TIME:  50 SEC
PACKAGING:  
MACHINE:  350 TON/150 ONLY

MOULD LOCATION:  
COMMENTS:  HYDRAULIC CORES
