PRODUCT DESCRIPTION
CUSTOMER:  AGRIGEL
PART NAME:  FILTER CAP/TOPS 
PART NUMBER:  LFF102
MATERIAL:  30% GLASS FILLED POLYPROPYLENE
SUPPLIER:  PLASTAMID/AP
MATERIAL CODE: PH2120 
COLOUR:  BLACK
 PIGMENT NUMBER AND SUPPLIER:  HBL315MB MERCURY
WEIGHT:  156.5 G
NUMBER OF CAVITIES:  1
CYCLE TIME:  60 SEC
PACKAGING:  
MACHINE: 150/350

MOULD LOCATION:  
COMMENTS:  HYDRAULIC CORES
