PRODUCT DESCRIPTION
CUSTOMER:  AGRIGEL
PART NAME:  FILTER SEAL
PART NUMBER:  LFF105
MATERIAL:  MONPRENE
SUPPLIER:  ADVANCED POLYMERS
MATERIAL CODE:   1527 NATURAL
COLOUR:  BLACK
 PIGMENT NUMBER AND SUPPLIER:  HBL315MB MERCURY
WEIGHT:  6 G
NUMBER OF CAVITIES:  1
CYCLE TIME:  30 SEC
PACKAGING:  
MACHINE:  20 TON +

MOULD LOCATION:  
COMMENTS:  
