PRODUCT DESCRIPTION
CUSTOMER:  AGRIGEL
PART NAME:  BLUE LDPE FLOAT BODY
PART NUMBER: LFM103
MATERIAL:  HIDENSITY POLYETHEYLENE 
SUPPLIER:  ADVANCED POLYMERS
MATERIAL CODE:   HD6600B
COLOUR:  BLUE
 PIGMENT NUMBER AND SUPPLIER:  MP8212MB
WEIGHT:  10.0 G
NUMBER OF CAVITIES:  2
CYCLE TIME:  30 SEC
PACKAGING:  
MACHINE:  20 TON

MOULD LOCATION:  
COMMENTS:  
