PRODUCT DESCRIPTION
CUSTOMER:  AGRIGEL
PART NAME:  PISTON SLEEVE WITH BRASS INSERT
PART NUMBER: LFP – 1011 - 2
MATERIAL:  MOLY FILLED ACETAL
SUPPLIER:  PLASTOMARK
MATERIAL CODE:  C9012M
COLOUR:  NATURAL
 PIGMENT NUMBER AND SUPPLIER:  
WEIGHT:  26G
NUMBER OF CAVITIES:  2
CYCLE TIME:  40 SEC
PACKAGING:  
MACHINE: 90 TON +

MOULD LOCATION:  
COMMENTS:  USES ONE 8MM AND ONE 10MM BRASS INSERTS
