PRODUCT DESCRIPTION
CUSTOMER:  AGRIGEL
PART NAME:  CENTRE SECTIONS ONLY
PART NUMBER:  LFP1001
MATERIAL:  30% GLASS FILLED POLYPROPYLENE
SUPPLIER:  PLASTAMID/AP
MATERIAL CODE:  PH2120
COLOUR:   GREEN
 PIGMENT NUMBER AND SUPPLIER: JP6089 PM
WEIGHT:  460 G
NUMBER OF CAVITIES:  1
CYCLE TIME:  3 MIN
PACKAGING:  
MACHINE:  350 TON ONLY

MOULD LOCATION:  
COMMENTS:  LOOSE CORES WATCH FOR CRACKING
USES CENTRE SECTION SLEEVES
