PRODUCT DESCRIPTION
CUSTOMER:  AGRIGEL
PART NAME:  CONCERTINA DIAPHRAGM
PART NUMBER:  LFP1014
MATERIAL:  HYTREL
SUPPLIER:  PLASTAMID
MATERIAL CODE:  G4074(PREFERED)/4056
COLOUR:  NATURAL
 PIGMENT NUMBER AND SUPPLIER:  
WEIGHT:  11.5 G
NUMBER OF CAVITIES:  2
CYCLE TIME:  60 SEC
PACKAGING:  
MACHINE:  150 TON/120 TON

MOULD LOCATION:  
COMMENTS:  MIX AS FOLLOWS: TEN SPOONS FINI WAX (supplied by Chemfit) + 1 CAP FULL LIQUID PARAFIN PER 2KG HYTREL
