PRODUCT DESCRIPTION
CUSTOMER:  AGRIGEL
PART NAME:  BACK DIAPHRAGM OUTER RING
PART NUMBER:  LFP1020
MATERIAL:  30 % GLASS FILLED POLYPROP
SUPPLIER:  PLASTAMID/AP
MATERIAL CODE: PH2120 
COLOUR:  GREEN
 PIGMENT NUMBER AND SUPPLIER:  JP6089
WEIGHT:  3G
NUMBER OF CAVITIES:  1
CYCLE TIME:  20 SEC
PACKAGING:  
MACHINE: 20TON

MOULD LOCATION:  
COMMENTS:  USED FOR OVERMOULDING IN BACK DIAPHRAGM/PISTON DIAPHRAGM
