PRODUCT DESCRIPTION
CUSTOMER:  AGRIGEL
PART NAME:  END COVER
PART NUMBER:  LFP1022
MATERIAL:  30 % GLASS FILLE POLYPROP
SUPPLIER:  PLASTAMID/AP
MATERIAL CODE:   PH2120
COLOUR:  GREEN
 PIGMENT NUMBER AND SUPPLIER:  JP6089
WEIGHT:  31 G
NUMBER OF CAVITIES:  2
CYCLE TIME:  30 SEC
PACKAGING:  
MACHINE: 90 TON +
MOULD LOCATION:  
COMMENTS:  
