PRODUCT DESCRIPTION
CUSTOMER:  AGRIGEL
PART NAME:  CHECK VALVE BODY CAGE (TOP + BOTTOM) (BIRD CAGE)
PART NUMBER:  LFP1027
MATERIAL:  30% GLASS FILLED POLYPROP
SUPPLIER:  PLASTAMID/AP
MATERIAL CODE:  PH2120
COLOUR:  GREEN
 PIGMENT NUMBER AND SUPPLIER:  JP6089
WEIGHT:  5 G
NUMBER OF CAVITIES:  4
CYCLE TIME:  30 SEC
PACKAGING:  
MACHINE: 90 TON +

MOULD LOCATION:  
COMMENTS:  
